## Slide 1: Circuit QED Experiment
Peng Zhou
Zi-Jin Lei

## Slide 2: Nature, Vol431, September2004, 162-167

## Slide 3: Outline
Motivation: (Peng)
  Why Circuit QED?
  What is strong coupling and how to testify?
Methods and Difficulties: (Zi-Jin)
  Sample fabrication
  Measurement techniques
Measurements and Results (Peng)
Summary(both)

## Slide 4: Motivation
Highly polarizable artificial atom  large dipole moment
Comparison between dipole of SC and Ryderberg atom
Small size of 1D cavity  large field strength
Strong coupling limit

## Slide 5: Cooper Pair Box: Qubit Engineering
Artificial atom
Qubit Hamiltonian in basis
Two level system in basis
Band Structure
Electrostatic energy in absence of
Josephson tunneling
Tunneling lifts the degeneracy
fabrication
fabrication
In situ
In situ
Notes: Overall scale engineered during fabrication
Further tuned in situ electrically

## Slide 6: Strip line resonator
Operating Temperature: ~20mK
  Superconducting, no dissipation
  Microwave (~6GHz) photon energy larger than thermal photon
1D waveguide
Dissipation
(maybe more properties to be added )

## Slide 7: Zi-Jin: Methods and Difficulties
  Cavity and CPB fabrication
  Measurement techniques
    Dilution refrigerator
    Sub-in-situ amplifier at 1K
    Phase lock-in tech
    The realization of single photon

## Slide 8: How to fabricate a microwave cavity?
Optical lithography
Silicon Substrate, Niobium film cavity
Quasi one dimensional coplanar cavity
The shape is meandered
To meet the requirements
  Si is transparent for microwave, low dissipation, Qint ~ 10 6
  Size: d1 = μm, d2 = μm, Ersm = 0.2 V/m
  Z = 50 Ω, impendence match to Microwave Components
  Tc(Nb) = 9.26K, Tc (Al) = 1.20K, superconducting

## Slide 9: How to fabricate a microwave cavity?
Cross section of transm. Line, TEM mode

## Slide 10: How to fabricate CPB
Aluminum-oxidation-aluminum structure
Coupling to cavity, connecting to ground
Sub-micrometer size structure: Electron beam lithography
EJ is controlled by the depth of oxidation layer
Double angles deposition

## Slide 11: How to fabricate CPB
Aluminum-oxidation-aluminum structure
Coupling to cavity, connecting to ground
Sub-micrometer size structure: Electron beam lithography
EJ is controlled by the depth of oxidation layer
Double angles deposition

## Slide 12: Measurement Technique
Low temperature tech
Sub-in-situ amplification
Microwave technique
Small signal analysis

## Slide 13: Dilution Refrigerator

## Slide 14: Dilution Refrigerator

## Slide 15: Dilution refrigerator

## Slide 16: RF amplifier at 1K
No thermal excitation of electron-hole pairs
Mature High Electron Mobility Transistor (HEMT)
Low noise
Luckily, you can buy it!
Cross-sectional STEM image of the gate region in a 130-nm InP, from IEEE ELECTRON DEVICE LETTERS, VOL. 33, NO. 5, MAY 2012

## Slide 17: Phase lock-in tech
the orthogonality of sine functions
Collect out the signal even 1000 less than noise

## Slide 18: The realization of single photon
To be added

## Slide 19: Dispersive Readout: Why Ng = 1?
First order decoupled from 1/f noise
Dispersive is the most sensitive (high SNR)

## Slide 20: 1/f noise sensitivity
To be added

## Slide 21: Transmission Power and Phase Spectrum
Probe the resonator system spectroscopically
Far-detuned qubit qubit and resonator are decoupled
Dispersive QND readout at e.g.
Notes: Question: why shift the experimental data by +- Vr? Is this QND measurement?  yes
Why the peak is not at 6.044GHz. Does that mean the resonator resonance frequency is still shifted?

## Slide 22: Measurements of phase shift vs.

## Slide 23: Measurements of phase shift vs.

## Slide 24: Vacuum Rabi Mode Splitting
Qubit at charge degeneracy
Combined ground state
Weak probe beam
Sensitive to photon number
Evidence for strong coupling

## Slide 25: Weak Beak: Why and How?
If n too large: maybe excite to large energy values
If n too small: cannot distinguish from thermal noise.
To be added: How?

## Slide 26: Vacuum Rabi Mode Splitting (cont'd)

## Slide 27: Summary
In situ control of qubit parameter
Transmission measurement
QND readout is possible
Strong coupling regime is achieved

## Slide 28: References
[1] Wallraff, Andreas, et al. "Strong coupling of a single photon to a superconducting qubit using circuit quantum electrodynamics." Nature 431.7005 (2004): 162-167.

## Slide 29: Appendix: Dilution refrigerator